## Slide 1: Practice 10 - Analysis of thermograms using the Proteus program, radiographs, diffractograms and the results of electron microscopic analysis of JEOL firing products 2 академических часа

## Slide 2: X-Ray Diffraction
One of the phenomena of interaction of X-rays with crystalline matter is its diffraction, produced by the reticular planes that form the atoms of the crystal. A crystal diffracts an X-ray beam passing through it to produce beams at specific angles depending on the X-ray wavelength, the crystal orientation and the structure of the crystal. In the macroscopic version of X-ray diffraction, a certain wavelength of radiation will constructively interfere when partially reflected between surfaces (i.e., the atomic planes) that produce a path difference equal to an integral number of wavelengths. This
condition is described by the Bragg law: 2d sin = n
where n is an integer, is the wavelength of the radiation, d is the spacing between surfaces and is the angle between the radiation and the surfaces. This relation demonstrates that interference effects are observable only when radiation interacts with physical dimensions that are approximately the same size as the wavelength of the radiation. Since the distances between atoms or ions are on the order of 10-10m (1Å), diffraction methods require radiation in the X-ray region of the electromagnetic spectrum, or beams of electrons or neutrons with similar wavelength. So, through X-ray spectra one can identify and analyse any crystalline matter. The degree of crystallinity or order will conditionate the quality of the obtained result. In order to do this, a diffractometer is needed.
Basically, an X-ray diffractometer consists in an Xray generator, a goniometer and sample holder and an X-ray detector, such as photographic film or a movable proportional counter. T
he most usually employed instrument to generate X-rays are X-ray tubes, which generate X-rays by bombarding a metal target with high energy (10-100keV) electrons that knock out core electrons. Thus, an electron in an outer shell fills the hole in the inner shell and emits an X-ray photon. Two common targets are Mo and Cu, which have strong K X-ray emissions at 0.71073 and 1.5418Å, respectively. Apart from the main line, other accompanying lines appear, which have to be eliminated in order to facilitate the interpretation of the spectra. These are partially supressed by using crystal monochromators.

## Slide 3: X-Ray Diffraction
The most interesting X-ray diffraction techniques for this work are those related to the analysis of polycrystalline materials and mainly of powders. In this case the powder
provides all the possible orientations of the small crystals giving rise to a large number of
diffraction cones, each one corresponding to a family of planes satisfying the Bragg’s law.
For large grains, rings are discontinuous and formed by small spots. As the size of the
grains diminishes, the spots are closer and for an optimum size a continuous ring is
obtained, which is transferred into a peak when working with graphic registers or lines in a
photographic register. For lower grain sizes the clarity of rings is lost again and wide peaks
or bands appear. When the crystals are not randomly but preferentially oriented, the
intensity of the different rings and along each ring is not uniform.

## Slide 4: X-Ray Diffraction
Quantitative analysis of diffraction profiles can be diverse. We will describe briefly
the measure of grain size in polycrystalline specimens that, as previously discussed, is a
crucial parameter in SGS.
The determination of the size of the crystals in a powder can be carried out thanks
to measurements that must be made on the profile of the diffraction peaks. One of the
functions that best describes the powder diffraction profiles is the Voigt function. This
consists in a convolution product of a Lorentzian and Gaussian function and allows to: 1)
Model size (Lorentzian component) and strain (Gaussian component) line-broadening
contributions simultaneously; 2) Separate instrumental and specimen contributions to the
diffracted line profile. Instrumental broadening is due to causes such as slit widths, sample
size, penetration in the sample, imperfect focusing, etc.

## Slide 5: X-Ray Diffraction

## Slide 6: Transmission Electron Microscopy
In 1925-27, Busch discovered that a rotationally symmetric, inhomogeneous
magnetic field could be conceived of as a lens for an electron beam. The use of electron
beams for producing enlarged images was first carried out in 1932 by Ernst Ruska and
Max Knoll and perfected microscopes could be mass-produced from the beginning of the
1950s. A simplified scheme of a TEM is shown in fig. 2.5.
One of the greatest advantages of the TEM is the excellent horizontal resolution
(i.e., the horizontal distance of two object details just separable from one another), because
it depends on the wavelength of the radiation employed, i.e., the smaller the wavelength
the greater the resolution. In TEM the incident radiation is a beam of electrons that has a
wavelength of the form: =
where V - is the acceleration voltage (in volts) applied to incident electrons.
The interaction between the incident beam and the sample is not only superficial,
but in a certain volume of the sample. This volume is greater at greater acceleration
potentials but is smaller at greater average atomic number of the sample.

## Slide 7
There is a great variety of TEM depending on its specific characteristics. We will
briefly describe:
CTEM (Conventional TEM) detects only the transmitted electrons.
HRTEM (High Resolution TEM) can detect electrons diffracted at a wide
range of angles.
These microscopes can also have a chemical detector in order to identify the
elements that are part of the sample. This is the most elemental TEM and its principles can also be extended to the other kinds of TEM.
One of the characteristics of the sample in order to provide a TEM image is that it
must be very thin because the electrons detected are those which cross the sample.
There are three basic parts in a TEM:
1) The gun, that is at the top of the microscope. It generates the accelerated
electron beam.
2) The vertical column, where the beam interacts with the sample and the
first images are formed.
3) The screen, where the final image is formed.
In the gun, the beams can be produced by three ways:
1) Thermal emission, where a filament is heated and emits electrons
because of the Joule effect. This is the most usual method in CTEM.
2) Indirect heating, where monocrystals of LaB6 or WZr are used as
filaments.
3) By field emission, where monocrystals of W with V-shape are used.
Schematic design of a transmission electron microscope. A) Ray path for bright
field imaging (three-stage magnification); b) Ray path for selected area diffraction (SAD).
The excitation of the intermediate lens is weaker in b) than in a): thus, the primary
diffraction pattern is imaged by the intermediate lens instead of the first-stead image